Influence of adsorbent composition and solution pH on heavy metal removal from aqueous solution using water treatment residuals from a groundwater treatment plant

Supplementary Information

Andrea Steuer1,2, Katharina Sperling2, Daniel Mahringer1, Aki S. Ruhl1,2

1Section II 3.3, German Environment Agency, Schichauweg 58, 12307 Berlin, Germany

2Water Treatment, Technische Universität Berlin, KF 4, Straße des 17. Juni 135, 10623 Berlin, Germany

Goodness of fit of kinetic and isotherm models

Goodness of fit of all models was evaluated using the Pearson correlation coefficient (R²), the sum of squared residuals (RSS), the chi-squared analysis (χ²) [1] and the Akaike information criterion (AIC) [2] given in formulas 7 to 10 in Table SI 1. The χ² becomes negative with negative q values, so an adjusted χ² was calculated with absolute q values in the denominator (formula 11).

Table SI 1: Calculation of different model goodness of fit descriptors

|  | Calculation | Variables | Formula |
| --- | --- | --- | --- |
| AIC | 2k-2ln⁡(Lmax) | k = number of estimated parameters Lmax= maximum value of the likelihood function in the model qe,m = modelled loading at equilibrium (mg/g) qe = experimental loading at equilibrium (mg/g) qe = mean of experimental loading values (mg/g) qe = absolute value of q (mg/g) | (7) |
| R² | (qe,m- qe)²(qe,m- qe)²+ (qe,m-qe)² |  | (8) |
| RSS | (qe- qe,m)² |  | (9) |
| χ2 | (qe- qe, m)²qe |  | (10) |
| χ2adj | (qe- qe, m)²qe |  | (11) |

Table SI 2: Model and goodness of fit parameters for adsorption kinetic of HM onto Fe-WTR at pH 7 in DW. Best fit is marked in bold.

| model | parameter | unit | As(III) | Cd(II) | Cu(II) | Ni(II) | Pb(II) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PFO | Qe,1 | mg/g | 38.53 | 7.80 | 71.14 | 0.00 | 79.96 |
|  | K1 | min-1 | 1.78∙10-2 | 1.10∙100 | 2.40∙10-1 | 9.56∙10-2 | 1.88∙100 |
|  | RSS |  | 1,885.36 | 260.49 | 2,623.53 | 557.23 | 198.11 |
|  | R² |  | 0.82 | 0.40 | 0.88 | 0.06 | 0.99 |
|  | Χ² * |  | 71.96 | 109.31 | 56.20 | -35.13 | 2.81 |
|  | Χ²adj * |  | 77.78 | 109.31 | 56.20 | 91.90 | 2.81 |
|  | AIC |  | 233.15 | 175.58 | 250.25 | 202.19 | 169.55 |
| PSO | Qe,2 | mg/g | 41.64 | 7.79 | 72.87 | 0.10 | 80.59 |
|  | K2 | mg/g/min | 5.22∙10-4 | 4.54∙10-1 | 6.40∙10-3 | 1.00∙10-7 | 6.18∙10-2 |
|  | RSS |  | 1394.75 | 269.99 | 1287.01 | 557.22 | 128.88 |
|  | R² |  | 0.86 | 0.38 | 0.93 | 0.06 | 0.99 |
|  | Χ² * |  | 55.76 | 123.50 | 25.40 | -35.12 | 1.88 |
|  | Χ²adj * |  | 63.96 | 123.50 | 25.40 | 91.90 | 1.88 |
|  | AIC |  | 223.20 | 176.83 | 226.03 | 202.19 | 154.08 |
| Elovich | α | mg/g/min | 4.15 | 100,000.00 | 10,197.62 | 0.01 | 100,000.00 |
|  | β | g/mg | 0.17 | 2.37 | 0.19 | 100.00 | 0.19 |
|  | RSS |  | 648.90 | 371.97 | 516.52 | 562.74 | 4,158.23 |
|  | R² |  | 0.92 | 0.34 | 0.97 | 0.06 | 0.85 |
|  | Χ² * |  | 5.83 | 132.37 | 10.09 | -38.49 | 53.82 |
|  | Χ²adj * |  | 67.40 | 132.37 | 10.09 | 93.01 | 53.82 |
|  | AIC |  | 197.95 | 188.05 | 194.99 | 202.54 | 279.14 |

* values q = 0 were excluded from calculation

Table SI 3: Model and goodness of fit parameters for adsorption kinetic of HM onto Mn-WTR at pH 7 in DW. Best fit is marked in bold.

| Model | Parameter | unit | As(III) | Cd(II) | Cu(II) | Ni(II) | Pb(II) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PFO | Qe,1 | mg/g | 34.70 | 46.72 | 82.56 | 30.21 | 85.26 |
|  | K1 | min-1 | 1.00∙10-3 | 2.48∙10-3 | 4.86∙10-3 | 1.03∙10-3 | 1.06∙10-1 |
|  | RSS |  | 303.31 | 863.27 | 2,028.03 | 855.91 | 1466.62 |
|  | R² |  | 0.95 | 0.94 | 0.95 | 0.85 | 0.95 |
|  | Χ² |  | 19.60 | 46.97 | 81.94 | -9.41 | 34.73 |
|  | Χ²adj |  | 23.16 | 46.97 | 81.94 | 65.60 | 34.73 |
|  | AIC |  | 164.68 | 197.10 | 223.58 | 196.84 | 213.53 |
| PSO | Qe,2 | mg/g | 41.33 | 50.68 | 86.67 | 35.94 | 87.38 |
|  | K2 | mg/g/min | 1.00∙10-3 | 2.48∙10-3 | 4.86∙10-3 | 1.03∙10-3 | 1.06∙10-1 |
|  | RSS |  | 209.45 | 709.15 | 1,111.00 | 835.40 | 481.66 |
|  | R² |  | 0.97 | 0.94 | 0.97 | 0.85 | 0.98 |
|  | Χ² |  | 13.72 | 35.87 | 45.70 | -9.82 | 13.86 |
|  | Χ²adj |  | 17.37 | 35.87 | 45.70 | 70.01 | 13.86 |
|  | AIC |  | 153.20 | 191.01 | 204.92 | 196.09 | 179.02 |
| Elovich | α | mg/g/min | 0.08 | 0.58 | 3.82 | 0.06 | 1,480.38 |
|  | β | g/mg | 0.11 | 0.12 | 0.08 | 0.11 | 0.15 |
|  | RSS |  | 158.91 | 692.46 | 1,019.06 | 869.78 | 1,584.67 |
|  | R² |  | 0.97 | 0.94 | 0.97 | 0.85 | 0.93 |
|  | Χ² |  | 7.72 | 26.79 | 17.89 | -10.03 | 31.30 |
|  | Χ²adj |  | 11.66 | 26.79 | 17.89 | 79.58 | 31.30 |
|  | AIC |  | 144.64 | 190.27 | 202.25 | 197.34 | 215.93 |

* values q = 0 were excluded from calculation

Table SI 4: Freundlich model and goodness of fit parameters of HM adsorption onto Fe-WTR and Mn-WTR.

| WTR | H2O | Analyte | pH | 1/n | KF | RSS | R² | Χ² | Χ²adj | AIC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fe | UW | As(III) | 6 | 0.47 | 1.77∙100 | 270.60 | 0.97 | -726.44 | 773.13 | 123.64 |
|  |  |  | 7 | 0.45 | 1.68∙100 | 239.29 | 0.96 | -63.16 | 111.20 | 120.94 |
|  |  |  | 8 | 0.29 | 3.77∙100 | 590.80 | 0.78 | -1,075.29 | 1,238.07 | 140.82 |
|  |  | Cd(II) | 6 | 11.49 | -4.27∙10-39 | 477.19 | 0.42 | 83.92 | 95.39 | 136.12 |
|  |  |  | 7 | 0.27 | 2.93∙100 | 372.48 | 0.70 | -105.60 | 275.67 | 130.67 |
|  |  |  | 8 | 0.20 | 9.75∙100 | 9,047.15 | 0.24 | -3,570.12 | 5,366.86 | 200.85 |
|  |  | Cu(II) | 6 | 0.28 | 1.13∙10-1 | 7,146.50 | 0.69 | -889.78 | 4,161.66 | 195.67 |
|  |  |  | 7 | 0.47 | 6.52∙100 | 3,414.49 | 0.93 | 3,144.99 | 10,686.80 | 179.42 |
|  |  |  | 8 | 0.10 | 1.52∙10-1 | 23,012.65 | 0.03 | -197.52 | 8,296.84 | 221.39 |
|  |  | Ni(II) | 6 | 0.65 | -1.05∙10-1 | 406.27 | 0.68 | -32.56 | 112.59 | 132.58 |
|  |  |  | 7 | 0.11 | 2.29∙100 | 374.71 | 0.05 | 137.46 | 253.98 | 130.81 |
|  |  |  | 8 | 0.06 | 7.16∙100 | 8,606.07 | 0.01 | 567.47 | 1,227.74 | 199.76 |
|  |  | Pb(II) | 6 | 0.48 | 1.83∙10-1 | 3,179.63 | 0.98 | -33,301.50 | 36,969.04 | 177.85 |
|  |  |  | 7 | 0.58 | 1.06∙10-1 | 8,803.57 | 0.92 | 6,959.29 | 12,876.58 | 200.25 |
|  |  |  | 8 | 0.30 | 1.50∙10-1 | 7,382.03 | 0.65 | -27,420.68 | 28,282.24 | 196.38 |
| Fe | DW | As(III) | 6 | 0.51 | 5.76∙10-1 | 126.27 | 0.94 | 16.59 | 79.36 | 92.15 |
|  |  |  | 7 | 0.84 | 3.73∙10-2 | 34.41 | 0.98 | 5.05 | 5.25 | 68.75 |
|  |  |  | 8 | 0.63 | 1.96∙10-1 | 54.77 | 0.96 | 5.03 | 15.48 | 82.91 |
|  |  | Cd(II) | 6 | 1.75 | 6.43∙10-6 | 96.00 | 0.40 | -3.54 | 24.56 | 87.21 |
|  |  |  | 7 | 0.82 | 2.76∙10-2 | 15.87 | 0.97 | 6.56 | 6.71 | 54.82 |
|  |  |  | 8 | 0.52 | 5.87∙10-1 | 69.66 | 0.96 | 306.22 | 306.22 | 81.44 |
|  |  | Cu(II) | 6 | 0.68 | 4.12∙10-1 | 448.06 | 0.96 | 29.93 | 29.93 | 124.94 |
|  |  |  | 7 | 0.69 | 6.18∙10-1 | 816.73 | 0.95 | 52.59 | 52.59 | 147.95 |
|  |  |  | 8 | 0.23 | 7.78∙10-1 | 4,454.56 | 0.24 | 1,427.37 | 1,427.37 | 185.27 |
|  |  | Ni(II) | 6 | 2.33 | 2.30∙10-8 | 481.45 | 0.03 | 14.59 | 62.84 | 126.38 |
|  |  |  | 7 | 4.60 | 7.62∙10-16 | 612.02 | 0.16 | -33.04 | 45.57 | 131.18 |
|  |  |  | 8 | 0.19 | 9.78∙10-1 | 457.78 | 0.05 | 224.15 | 309.57 | 125.37 |
|  |  | Pb(II) | 6 | 0.53 | 9.59∙100 | 1,676.39 | 0.98 | 6,110.27 | 9,435.79 | 163.77 |
|  |  |  | 7 | 0.39 | 1.64∙10-1 | 5,952.33 | 0.85 | 9,493.83 | 22,342.13 | 191.64 |
|  |  |  | 8 | 0.19 | 2.02∙10-1 | 9,175.35 | 0.31 | 35,166.09 | 35,166.09 | 201.16 |
| Mn | UW | As(III) | 6 | 0.64 | 1.91∙10-1 | 163.89 | 0.92 | 27.86 | 44.72 | 96.84 |
|  |  |  | 7 | 0.46 | 7.74∙10-1 | 177.05 | 0.90 | 348.79 | 525.87 | 106.37 |
|  |  |  | 8 | 0.31 | 1.52∙100 | 110.40 | 0.81 | -143.89 | 198.58 | 103.92 |
|  |  | Cd(II) | 6 | 0.21 | 4.72∙100 | 595.64 | 0.62 | -668.30 | 793.19 | 141.00 |
|  |  |  | 7 | 0.31 | 3.73∙100 | 526.21 | 0.87 | 10,328.14 | 11,466.27 | 148.21 |
|  |  |  | 8 | 0.28 | 6.18∙100 | 383.41 | 0.92 | -3,915.17 | 4,075.56 | 131.31 |
|  |  | Cu(II) | 6 | 0.37 | 5.72∙100 | 1,229.09 | 0.93 | 1,575.94 | 1,575.94 | 156.94 |
|  |  |  | 7 | 0.49 | 3.10∙100 | 701.26 | 0.97 | 99.48 | 99.48 | 155.10 |
|  |  |  | 8 | 0.10 | 8.59∙100 | 2,728.49 | 0.04 | 522.86 | 915.49 | 174.48 |
|  |  | Ni(II) | 6 | 0.27 | 2.49∙100 | 451.15 | 0.60 | 114.10 | 114.10 | 125.08 |
|  |  |  | 7 | 0.49 | 5.60∙100 | 432.47 | 0.78 | -90.22 | 129.01 | 143.50 |
|  |  |  | 8 | 0.32 | 3.00∙100 | 104.66 | 0.96 | 71.00 | 71.00 | 102.75 |
|  |  | Pb(II) | 6 | 0.42 | 1.37∙10-1 | 2,952.78 | 0.97 | 13,082.25 | 13,082.25 | 176.22 |
|  |  |  | 7 | 0.46 | 1.01∙10-1 | 2,473.65 | 0.97 | 1,100.29 | 1,100.29 | 185.36 |
|  |  |  | 8 | 0.27 | 1.40∙10-1 | 3,137.90 | 0.66 | 160,425.67 | 160,425.67 | 177.56 |
| Mn | DW | As(III) | 6 | 0.47 | 4.04∙10-1 | 92.33 | 0.86 | 76.73 | 84.96 | 99.99 |
|  |  |  | 7 | 0.61 | 1.05∙10-1 | 50.42 | 0.87 | 5.88 | 7.59 | 86.68 |
|  |  |  | 8 | 0.61 | 1.34∙10-1 | 60.86 | 0.90 | 12.16 | 14.86 | 90.82 |
|  |  | Cd(II) | 6 | 0.34 | 9.16∙10-1 | 475.37 | 0.35 | -14.55 | 100.02 | 126.12 |
|  |  |  | 7 | 0.45 | 6.67∙10-1 | 181.69 | 0.84 | 14.85 | 83.06 | 106.89 |
|  |  |  | 8 | 0.58 | 3.92∙10-1 | 190.12 | 0.91 | 9.94 | 22.97 | 107.80 |
|  |  | Cu(II) | 6 | 0.44 | 1.95∙100 | 473.64 | 0.92 | 54.70 | 54.70 | 135.96 |
|  |  |  | 7 | 0.57 | 8.36∙10-1 | 501.66 | 0.94 | 26.94 | 26.94 | 137.22 |
|  |  |  | 8 | 0.34 | 2.82∙100 | 2,372.13 | 0.32 | 172.78 | 172.78 | 171.40 |
|  |  | Ni(II) | 6 | 0.48 | 2.12∙10-1 | 24.72 | 0.85 | 30.49 | 39.18 | 67.00 |
|  |  |  | 7 | 0.55 | 1.73∙10-1 | 18.43 | 0.94 | 0.24 | 5.73 | 61.12 |
|  |  |  | 8 | 0.71 | 7.67∙10-2 | 51.90 | 0.92 | 12.95 | 16.13 | 81.83 |
|  |  | Pb(II) | 6 | 0.45 | 9.43∙100 | 2,314.90 | 0.96 | 126.05 | 6,111.79 | 170.87 |
|  |  |  | 7 | 0.28 | 1.30∙10-1 | 6,906.65 | 0.62 | -2,308.35 | 4,418.78 | 194.92 |
|  |  |  | 8 | 0.11 | 1.35∙10-1 | 9,551.04 | 0.04 | -4,634.43 | 6,580.14 | 202.05 |

Table SI 5: Langmuir model and goodness of fit parameters of HM adsorption onto Fe-WTR and Mn-WTR.

| WTR | H2O | Analyte | pH | qmax | KL | RSS | R² | Χ² | Χ²adj | AIC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fe | UW | As(III) | 6 | 77.68 | 1.71∙10-3 | 374.76 | 0.96 | 15.67 | 22.49 | 130.81 |
|  |  |  | 7 | 60.23 | 2.12∙10-3 | 85.90 | 0.99 | 3.98 | 8.49 | 98.40 |
|  |  |  | 8 | 32.74 | 8.69∙10-3 | 214.26 | 0.93 | 1.84 | 14.27 | 118.51 |
|  |  | Cd(II) | 6 | -0.17 | -3.71E∙10-4 | 398.12 | 0.51 | 55.56 | 67.14 | 132.14 |
|  |  |  | 7 | 21.40 | 1.05∙10-2 | 170.07 | 0.88 | 8.86 | 14.05 | 113.43 |
|  |  |  | 8 | 42.21 | 3.03∙10-2 | 6,621.84 | 0.46 | 51.03 | 299.52 | 193.99 |
|  |  | Cu(II) | 6 | 86.68 | 1.46∙10-2 | 4,205.35 | 0.84 | -105.53 | 312.31 | 184.00 |
|  |  |  | 7 | 173.63 | 6.49∙10-3 | 1,909.01 | 0.97 | 130.00 | 2,364.11 | 166.63 |
|  |  |  | 8 | 35.63 | 1.12∙10-1 | 19,609.73 | 0.15 | -981.11 | 2,234.55 | 217.87 |
|  |  | Ni(II) | 6 | -30.34 | 5.36∙10-4 | 353.98 | 0.72 | -58.08 | 70.37 | 129.55 |
|  |  |  | 7 | 5.71 | 3.29∙10-2 | 322.12 | 0.18 | 1.80 | 136.13 | 127.48 |
|  |  |  | 8 | 13.91 | 4.35∙10-2 | 8,115.66 | 0.05 | -279.82 | 552.38 | 198.46 |
|  |  | Pb(II) | 6 | 291.35 | 2.24∙10-2 | 2,555.10 | 0.98 | -2,288.45 | 2,579.64 | 173.04 |
|  |  |  | 7 | 290.50 | 1.48∙10-2 | 10,370.56 | 0.91 | 4,907.88 | 6,691.71 | 203.86 |
|  |  |  | 8 | 76.18 | 1.26∙10-1 | 3,345.45 | 0.83 | -5,898.99 | 6,254.82 | 178.97 |
| Fe | DW | As(III) | 6 | 38.87 | 1.59∙10-3 | 80.42 | 0.96 | 5.98 | 6.95 | 84.03 |
|  |  |  | 7 | 96.23 | 1.48∙10-4 | 36.54 | 0.98 | 5.84 | 5.90 | 69.83 |
|  |  |  | 8 | 39.39 | 7.07∙10-4 | 54.10 | 0.97 | 3.30 | 3.48 | 82.66 |
|  |  | Cd(II) | 6 | 2.80 | -1.40∙10-3 | 64.12 | 0.65 | 16.50 | 29.70 | 79.95 |
|  |  |  | 7 | 54.53 | 1.75∙10-4 | 16.90 | 0.97 | 7.31 | 7.36 | 55.95 |
|  |  |  | 8 | 35.48 | 1.91∙10-3 | 40.47 | 0.98 | 4.51 | 4.51 | 71.66 |
|  |  | Cu(II) | 6 | 127.62 | 6.47∙10-4 | 384.52 | 0.97 | 23.99 | 23.99 | 121.88 |
|  |  |  | 7 | 168.97 | 7.65∙10-4 | 747.54 | 0.96 | 37.24 | 37.24 | 146.00 |
|  |  |  | 8 | 40.23 | 1.78∙10-2 | 3,076.36 | 0.44 | 1,219.78 | 1,219.78 | 177.12 |
|  |  | Ni(II) | 6 | 2545.78 | 3.10∙10-7 | 482.98 | 0.02 | 15.50 | 71.35 | 126.44 |
|  |  |  | 7 | 1.92 | -1.19∙10-3 | 60.69 | 0.91 | -28.29 | 79.17 | 84.96 |
|  |  |  | 8 | 3.97 | 2.43∙10-2 | 444.36 | 0.07 | -6.89 | 42.49 | 124.78 |
|  |  | Pb(II) | 6 | 286.97 | 8.29∙10-3 | 1,627.97 | 0.99 | 199.65 | 606.06 | 163.12 |
|  |  |  | 7 | 139.46 | 4.18∙10-2 | 1,739.74 | 0.96 | 70.53 | 1,880.25 | 164.58 |
|  |  |  | 8 | 57.98 | 3.05E∙10-1 | 4,493.27 | 0.65 | 6,172.35 | 6,172.35 | 185.46 |
| Mn | UW | As(III) | 6 | 69.35 | 3.03∙10-4 | 201.68 | 0.91 | 39.67 | 40.02 | 100.58 |
|  |  |  | 7 | 30.44 | 2.27∙10-3 | 138.73 | 0.93 | 13.30 | 14.74 | 101.49 |
|  |  |  | 8 | 15.74 | 6.29∙10-3 | 39.45 | 0.94 | 2.20 | 3.48 | 81.28 |
|  |  | Cd(II) | 6 | 20.81 | 3.90∙10-2 | 431.34 | 0.76 | 6.07 | 38.91 | 133.90 |
|  |  |  | 7 | 38.33 | 6.44∙10-3 | 581.83 | 0.89 | 78.13 | 79.33 | 150.62 |
|  |  |  | 8 | 42.94 | 1.80∙10-2 | 124.40 | 0.98 | -8.62 | 23.38 | 106.55 |
|  |  | Cu(II) | 6 | 91.98 | 6.23∙10-3 | 850.88 | 0.96 | 125.37 | 125.37 | 148.85 |
|  |  |  | 7 | 126.37 | 2.88∙10-3 | 747.89 | 0.97 | 45.13 | 45.13 | 156.65 |
|  |  |  | 8 | 17.16 | 2.14E∙10-1 | 2,101.63 | 0.22 | -27.71 | 430.86 | 168.74 |
|  |  | Ni(II) | 6 | 19.77 | 8.76∙10-3 | 357.83 | 0.73 | 18.46 | 18.46 | 120.44 |
|  |  |  | 7 | 44.99 | 6.06∙10-4 | 528.75 | 0.79 | -21.34 | 117.95 | 148.33 |
|  |  |  | 8 | 30.94 | 8.21∙10-3 | 144.67 | 0.95 | 9.19 | 9.19 | 109.87 |
|  |  | Pb(II) | 6 | 206.08 | 1.67∙10-2 | 2,787.18 | 0.97 | 1,935.37 | 1,935.37 | 174.95 |
|  |  |  | 7 | 191.01 | 1.49∙10-2 | 1,340.93 | 0.98 | 131.09 | 131.09 | 170.66 |
|  |  |  | 8 | 59.76 | 1.40∙10-1 | 656.08 | 0.93 | 52,004.33 | 52,004.33 | 143.13 |
| Mn | DW | As(III) | 6 | 19.57 | 1.52∙10-3 | 85.06 | 0.88 | 10.71 | 10.96 | 98.19 |
|  |  |  | 7 | 21.66 | 5.28∙10-4 | 59.13 | 0.87 | 8.58 | 8.87 | 90.18 |
|  |  |  | 8 | 22.93 | 7.73∙10-4 | 47.10 | 0.92 | 7.29 | 7.66 | 85.18 |
|  |  | Cd(II) | 6 | 8.79 | 2.29∙10-2 | 537.86 | 0.26 | -55.11 | 74.97 | 128.59 |
|  |  |  | 7 | 27.50 | 1.51∙10-3 | 261.82 | 0.81 | 65.34 | 65.74 | 114.20 |
|  |  |  | 8 | 48.52 | 9.03∙10-4 | 255.35 | 0.89 | 26.57 | 27.80 | 113.70 |
|  |  | Cu(II) | 6 | 62.32 | 2.76∙10-3 | 222.68 | 0.97 | 8.96 | 8.96 | 119.36 |
|  |  |  | 7 | 87.75 | 1.13∙10-3 | 654.36 | 0.93 | 35.80 | 35.80 | 143.07 |
|  |  |  | 8 | 32.93 | 7.38∙10-3 | 1,856.80 | 0.45 | 118.36 | 118.36 | 166.02 |
|  |  | Ni(II) | 6 | 11.57 | 1.24∙10-3 | 34.63 | 0.83 | 18.85 | 18.98 | 73.74 |
|  |  |  | 7 | 16.91 | 1.04∙10-3 | 20.19 | 0.94 | 2.74 | 3.08 | 62.94 |
|  |  |  | 8 | 32.58 | 5.14∙10-4 | 44.91 | 0.93 | 13.08 | 13.60 | 78.94 |
|  |  | Pb(II) | 6 | 194.07 | 9.03∙10-3 | 1,027.18 | 0.99 | -217.47 | 772.54 | 152.99 |
|  |  |  | 7 | 82.00 | 3.29∙10-2 | 2,246.83 | 0.88 | -416.11 | 625.76 | 170.21 |
|  |  |  | 8 | 31.42 | 1.21∙10-1 | 7,283.55 | 0.23 | -1,289.91 | 1,613.43 | 196.08 |

References

[1] B. Boulinguiez, P. Le Cloirec, D. Wolbert, Revisiting the determination of langmuir parameters—Application to tetrahydrothiophene adsorption onto activated carbon, Langmuir 24 (2008) 6420–6424, doi:10.1021/la800725s.

[2] H. Akaike, Akaike’s Information Criterion, in: M. Lovric (Ed.), International Encyclopedia of Statistical Science, Springer Berlin Heidelberg, Berlin, Heidelberg, 2011, doi:10.1007/978-3-642-04898-2_110.